Uses of TCP-95g (Tricalcium phosphate)

for substitution of small bone defects

(instruction for administration)

Preparations

Round (or irregular shaped) granules of TCP-95g of white or close to white colour. Composition - 5% of hydroxyapatite and 95% of tricalcium phosphate.

The material is produced in granular form with the sizes between 0,25 and 2 mm. Granules are porous ceramic fragments.

TCP-95g is part of inorganic hard tissues matrix. It has better human tissues biocompatibility and does not cause rejection reaction. It differs more in accelerated bio disruptiveness from hydroxyapatite, after the bone cavity filling the material resorbs being substituted by osseous tissue.

Treatment

The material is recommended for filling of small bone defects of different etiology after surgical treatment in cases of cystectomy, resection and extraction of teeth, for prevention of alveolar process atrophy, etc.

Uses

The material TCP-95g in granular form is moistened by the patient’s blood or better by the mixture of blood with bone marrow (on sterile physiologic solution) and by a surgical instrument is inserted into the osseous defect filling up to 70-80% of the cavity. Fresh bleeding may be caused by dental bur passing cortical layer of the bone. The defect is closed by soft tissues with stitching them not in immediate proximity to TCP-95g.

Antibiotics, immunomodulators and other medicines can be applied with TCP-95g by impregnation before use.

Sterilization

Sterilization of the material should be made before the product application and can be made repeatedly in an autoclave not less than 30 min. For this purpose the material should be placed in packing not skipping of a steam (moisture).

Contraindications

Pus inflammatory processes in the area with the defect planned for filling.

Proprietary preparations

The product is available in 1 g sterile packing; 5 g, 50 g packing are not sterilized.

Storage

To store in a dry place at room temperature.

JSC “R&P Org. “POLYSTOM” (Bolshaya Semenovskaya str, 40, Moscow, 107023, Russian Federation, Tel./Fax: +7(495) 737-68-92, 967-99-38, www.polystom.ru)

Batch number 	                 Product sterility              Manufacturing date

Product manufacturer               Best before               Pay attention to the instruction

The product is intended for single use            Pay attention to the associated documents